## Slide 1
Three mistakes we have made during fabrication of quantum dots solar cell; How can you learn from them
Saifful Kamaluddin bin Muzakir
saifful@ump.edu.my / 019 276 3844

## Slide 2: State of the Art
GaAs
c-Si
CIGS/a-Si
Dye
Quantum Dots
Theoretical PV conversion efficiency of 1 cell
32%
>60%
Experimental PV conversion efficiency of 1 cell
11%
32%
32%
32%
13%
21%
28%
29%
Source: National Renewable Energy Laboratory
1st Generation
Crystalline Solar Cells
Commercial
2nd Generation
Thin Film Solar Cells
Commercial
3rd Generation
Molecular Absorber Solar Cells
Research

## Slide 3: Device Structure
R
O
H
P
O
R
O
U
L
F
E
A. DSSC
B. QDSC with ligand
C. QDSC without ligand
Dye
QD
Ligand
QD
Conducting glass
Conducting glass
Working electrode
Counter electrode
Liquid electrolyte
TiO2
TiO2
TiO2
Muzakir et al. 2013. Physical Chemistry Chemical Physics. 15:16275-16285.

## Slide 4: Working Principle
R
O
H
P
O
R
O
U
L
F
h
e
e
e
h
e
e
e
e
e
e
e
e
e
E
h
e
e
e
e
e
e
External Circuit
TiO2
TiO2
TiO2
Dye
ligand
QD
QD
excitation
A. DSSC
B. QDSC with ligand
C. QDSC without ligand
VOC
HOMO
LUMO
Muzakir et al. 2013. Physical Chemistry Chemical Physics. 15:16275-16285.

## Slide 5: Size of QDs vs. performance of QDSC
The yielded IPCE (boxes) and PCE (circles) by fabricated cell using respective CdSe QDs size

## Slide 6: CdSe QDs synthesis: Organometallic vs Microemulsion
Narrow size distributions
of small QDs
Wurtzite P63mc crystal structure
Wurtzite P63mc crystal structure
Wide size distributions of big QDs
4 h at 23 °C
64 h at 23 °C
169 h at 23 °C
5 h at 50 °C
After 24 h cooling
1 min at 37 °C
5 min at 37 °C
10 min at 37 °C
15 min at 37 °C
30 min at 37 °C
60 min at 37 °C
120 min at 37 °C

## Slide 7: DFT: Realistic cluster modeling
(CdSe)13

## Slide 8: Realistic Cluster Models
(CdSe)6
(CdSe)13
(CdSe)16
(CdSe)32
(CdSe)26
Muzakir et al. 2013. Physical Chemistry Chemical Physics. 15:16275-16285.

## Slide 9: Mistake #1: The best size
CBD
(CdSe)26 - TiO2
~(CdSe)26
(CdSe)13
CdSe - TiO2
~73%
~53%
1.90 nm
~(CdSe)32
~39%
(CdSe)32 - TiO2
Direct Attachment
7.76 nm
SILAR
(CdSe)13
1.90 nm
~73%
(CdSe)13 - TiO2
3.02 nm

## Slide 10: Mistake #2: Ligand usage
(CdSe)z-MPA-TiO2
~19%
Ligand Assisted
~(CdSe)32
(CdSe)z-MSA-TiO2
~33%
Ligand Assisted
~(CdSe)32
(CdSe)13
-4.188 eV
-6.529 eV
MPA
-3.63 eV
-7.14 eV
(CdSe)13
-4.188 eV
-6.529 eV
MAA
-3.61 eV
-7.11 eV

## Slide 11: Mistake #3: Size distribution
1.50 nm
1.90 nm
2.02 nm
2.44 nm
(CdSe)6
-4.020 eV
-6.495 eV
(CdSe)13
-4.188 eV
-6.529 eV
(CdSe)16
-4.208 eV
-6.438 eV
(CdSe)26
-4.993 eV
-6.950 eV
500 nm
530 nm
556 nm
634 nm
Narrow size distribution
CdSe - TNRs
~100%
~19%
Wide size distribution
TiO2
-4.200 eV
-7.200 eV

## Slide 12: Conclusion
Efficient injection
The best size
Suitable ligand
Narrow size distribution

## Slide 13: Electron injection efficiency
CdSe
LUMO
HOMO
h
e
e
PL intensity
Wavelength (nm)
Detector
Screen
TiO2
C.B.
V.B.
CdSe
LUMO
HOMO
h
e
e
PL intensity
Wavelength (nm)
e
PL intensity
Wavelength (nm)
100 %
Nonradiative
Notes: To harvest these excited state electrons, QDs are adsorbed onto the MOS surface.
In the QDs-MOS conjugate, upon absorption of photon with sufficient energy, the excited state electron has two options; (i) first is to recombine with hole in HOMO and (ii) second is to be injected into the lower lying LUMO energy level of MOS.
If all electron recombine into the HOMO, the PL intensity will be the same as the PL of bare QDs.
If all electron injected into the LUMO of MOS, the PL intensity is totally quenched.
Therefore, efficient electron injection is indicated by high percentage of PL intensity quenching in QD-MOS conjugates; in comparison with the PL intensity of the bare QDs.
The electron injection efficiency from QDs to MOS was quantitatively measured using photoluminescence spectroscopy.
In bare QDs, upon absorption of photon with sufficient energy, electron in the HOMO is excited to LUMO energy level leaving hole at the HOMO.
The electron then recombine with the hole in the HOMO thus produces photon.
This photon is detected by photoluminescence spectrometer and PL intensity vs wavelength plot is produced. The intensity of PL depends on the number of recombination. The more excited state electron recombines to the HOMO, the higher the PL intensity would be.